## Slide 1
Vytvořeno z rozpočtu FOND VĚDY 2016
FV 16-11, Ing. KAMIL NOVÁK, prof. Ing. Jiří Burša, Ph.D.
1/XY
ÚSTAV MECHANIKY TĚLES, BIOMECHANIKY
A MECHATRONIKY
Model Yeoh
It is based on the Mooney-Rivlin polynomial formulation
Yeoh (1993) has shown that the total strain energy is more influenced by increments
than by ; thus it is proposed in the following form:
+
Later it was expanded with higher order terms to increase its progressivity.

## Slide 2
Exponential model - Delfino
where: a, b, d are material parameters, is modified first invariant of the right Cauchy-Green deformation tensor, J is third invariant of deformation gradient tensor. The original incompressible form of the model was proposed by Demiray*).
Exponential Fung-type model has its simplest form
and c, ci are material parameters, εi are components of Green-Lagrange strain tensor. The above shape neglects radial strain, its expanded formulation is needed to consider it, for instance
where
*) Demiray, H., "A note on the elasticity of soft biological tissues", Journal of Biomechanics 5, pp. 309-311, 1972
Due to application of the invariant the model is isotropic.
This model is orthotropic. Both models are purely phenomenological.
Hyperelastic models based on exponential functions

## Slide 3: Hyperelastic models based on exponential functions
Orthotropic exponential model Choi-Vito*)
It exploits another form of exponential functions of strain components:
where: C, bi are material parameters, εi are principal components of Green-Lagrange strain tensor (it assumes negligible impact of angular strains and also of radial strains on the SEDF).
Compared to Fung-type and Demiray models, this model summarizes the exponential functions specifying contributions of individual strain components, while Fung and Demiray models in fact multiply these contributions.
Therefore, Choi-Vito model gives lower increase of SEDF values at multiaxial stresses against the values at uniaxial stress.
*) Choi, H. S. , & Vito, R. (1990). Two-dimensional stress-strain relationship for canine pericardium. Journal of Biomechanical Engineering, 112 , 153–159 .

## Slide 4
10/25
ÚSTAV MECHANIKY TĚLES, BIOMECHANIKY
A MECHATRONIKY
c – material parameter [Pa] defines the slope of the curve
c1, c2, c3 – dimensionless parameters
Ei – components of Green-Lagrange strain tensor
This model also neglects the radial strain.
x
y
ln(x)
ln(1-x)
ln(1-x2)
-ln(1-x2)
asymptote of function
(in x=1 for such formulation)
Hyperelastic models based on other functions
Orthotropic logarithmic model Takamizawa-Hayashi (1987)
With respect to the character of stress-strain curves of soft tissues, a (modified) logarithmic function can be also used. Squared strains ensure the SEDF to be positive also in compression.
where