## Slide 1: Model Klosner-Segal
represents a modification of the Mooney-Rivlin model, which is unstable at soft tissues, especially at arteries. It may give results out of physical reality for multiaxial stress states for which testing is difficult or even hardly feasible. The effort to improve the description of soft tissues with polynomial models led to limitation to some members only. Model Klosner-Segal is given by the following equation:
where: cij are material parameters
= modified first invariant of right Cauchy-Green deformation tensor
= modified second invariant of right Cauchy-Green deformation tensor
It can be used in ANSYS or any other software with the 9-parameter Mooney-Rivlin model if we fit its parameters elsewhere.

## Slide 2: Fit of Klosner-Segal model for arteries
A least square fit (sum of residuals 9,91 kPa2) to the uniaxial experimental data (red rings): C11 = 372 kPa; C21 = -376 kPa; C22 = -250 kPa kPa; C23 = 324;
Warning: it should hold C11 + C21 > 0!!!

## Slide 3: Prediction of Klosner-Segal model for planar tension

## Slide 4: Other parameters of Klosner-Segal model
Another least square fit (sum of residuals 12,28 kPa2) to the same data (red rings):
C11 = 0.074 kPa; C21 = 29.11 kPa; C22 = -53.8 kPa; C23 = 292.3 kPa

## Slide 5: Predictions for planar and equibiaxial tension
The biaxial curves are not reasonable compared to the uniaxial data, they are too stiff.
Stress values from the uniaxial curve:
For λ= 1,3 => σ = 45 kPa;
for λ= 1,5 => σ = 180 kPa;
for λ= 1,7 => σ = 700 kPa.