## Slide 1: Poroelastic models of material with linear elastic solid phase and Newtonian liquid phase
In a certain range of flow capacities there is a linear dependence between pressure gradient and flow. This linearity is limited chiefly with transition to turbulent flow in pores, significant influence of surface stress, large strains of the solid phase and other non-linear effects.
Basic characteristics of a linear poroelastic material:
Porosity – (dimensionless) volume ratio of the fluid phase (pores) to the total volume of the porous material. It cannot specify the material permeability.
Specific permeability kapp [m4N-1s-1] – it represents a ratio of the volume flow through a unit cross section of the specimen in a defined direction within a time unit under unit pressure gradient. It depends on the viscosity of the fluid in the porous material – applied in experimental evaluation of material permeability.
Intrinsic permeability kf = kapp .η [m2] (η is dynamic viscosity of the liquid) – is independent of the viscosity, i.e. of the choice of the liquid in the porous material. Square root from the intrinsic permeability corresponds to the characteristic dimension of the pores in the in the solid phase (applicable for semi-permeable membranes).
Hydraulic conductivity kF = kapp .ρ .g [m/s] (ρ is mass density of the liquid and g is gravitational accelaration) – equals the flow velocity (calculated as flow per unit area) of a liquid through a porous material under unit dimensionless hydraulic gradient dp/(dx. ρ .g) – applicable for calculation of flow through a porous material (membrane).

## Slide 2: Darcy’s law
Under conditions of linear dependence of the liquid flow through a defined specimen cross section on the pressure gradient, it can be described by Darcy’s law as follows:
where q [m s-1] ─ is volume flow through a unit area per second,
kapp [m4N-1s-1] ─ is specific permeability,
p [Nm-2] ─ is pressure in the liquid.
For a steady flow through a homogenous prismatic (sealed on its circumference) specimen), the equation can be used in the following form:
where Q [m3s-1] ─ is the volume flow through the specimen per second,
A [m2] ─ is the specimen cross section,
Δp [Nm-2] ─ is difference of the pressures in front and behind the specimen,
Δ h [m] ─ is the specimen length in the flow direction.
Permeability of an arterial wall is on the order 10-16 [m4N-1s-1],
for intraluminal thrombus (ILT) it is in the range 10-12 – 10-14 [m4N-1s-1].

## Slide 3: Comparison of permeability with arterial resistence and impedance
Hydraulic resistance is defined for a steady flow as follows:
where Q [m3s-1] ─ is the volume flow per second,
Δp [Nm-2] ─ is difference of the input and output pressures.
For a pulsatile flow, the impedance (consisting of resistence, compliance and inertance) is represented by complex functions of angular frequency of pulsations
Permeability of an arterial wall [m4N-1s-1] is defined inversely to arterial impedance [Nsm-5].