## Slide 1: Constitutive models for large strain viscoelastic materials
Mathematical formulations of viscoelastic constitutive models under large strains are similar to hyperelastic formulations. However, the states of matter are typically out of thermodynamic equilibrium (non-equilibrium thermodynamics), thus Helmholtz free energy becomes the decisive quantity rather than the strain energy only. Its fomulation is: Ψ=W-TS where T is absolute temperature, S is entropy (both energies equal for elastic materials). This energy has a general formulation as follows:
where is the volume component of Helmholtz free energy, is its isochoric (deviatoric) component, is deviatoric part of right Cauchy-Green deformation tensor, J is the 3rd invariant of the deformation gradient tensor, is the set of functions describing the irreversible part of the Helmholtz free energy, Γα is a set of functions describing the time dependence of deformation. For the mathematical description, rheological models can be used similarly as in linear viscoelasticity. See the literature below for more details.
Simo, J.C., "On fully three-dimensional finite strain viscoelastic damage model: Formulation and computational aspects", Comput. Meth. In Appl. Mech. Eng., Vol. 60, pp. 153-173 (1987).
G.A. Holzapfel, "On large strain viscoelasticity: continuum formulation and finite element applications to elastomeric structures", Int. J. Numer. Meth. Eng., Vol. 39, pp. 3903-3926 (1996).