## Slide 1: Anisotropic structure-based models
They are used to describe behaviour of fibre composites with elastomer matrix (mostly rubber) reinforced with fibers. Their basic version assumes uniform ditribution of up to two families of perfectly aligned fibres with zero bending stiffness. In fact they assume an infinitesimal fibre diameter and are applicable for any extracellular fibres, having typically negligible bending stiffness.
Additional invariants of deformation gradient tensor are used to describe the contribution of fibres to the strain energy density. Invariants (or also „pseudo-invariants“) of the right Cauchy-Green deformation tensor C are mostly used and denoted with symbols I4 – I9. A modified form of the tensor, i.e. that limited to deviatoric part of deformation, is used here.
Similarly to isotropic elastomers, SEDF is decomposed into its volumetric part WV and deviatoric (isovolumic) part Wdev, which can be further decomposed into the isotropic contribution of the matrix Wiso and anisotropic contribution of fibres Waniso .
For the isotropic SEDF part Wiso , any suitable hyperelastic model can be used (neo-Hooke, Yeoh, ….), while for the pro anisotropic part Waniso exponential models are introduced most frequently for soft biological tissues. A and B represent here the so called „structural tensors“ defining directions of both fibre families.

## Slide 2: Model HGO (Holzapfel et al. 2000)
It is an anisotropic exponential model proposed for soft biological (e.g. arterial) tissues reinforced with two families of identical wavy fibres.
For the (isotropic) matrix, neo-Hookean model is used in its volumetric and deviatoric parts, while the anisotropic SEDF part Wanizo changes with respect to the sign of the respective invariants; due to fibre waviness, they apply only if the fibres are under tension. The mathematical formulation is as follows:
..... for
..... for
..... for
where: ..... for
c, k1, k2, d are material parameters,
are (pseudo)invariants of the right Cauchy-Green deformation tensor.
I4 and I6 are express squared stretches of both collagen fibre families.
J=det(F) is the third invariant of deformation gradient tensor F.
*) Holzapfel, Gasser,Ogden: A new constitutive framework for arterial wall mechanics, Journal of Elasticity, 2000. Originally formulated by Lanir Y: A structural theory for the homogeneous biaxial stress-strain relationships in flat collagenous tissues. J Biomech 1979,Vol. 12, pp. 423-436.
εx

## Slide 3: Model GOH (Gasser et al. 2006)
This model is the first one of the so called microfibre models. They are based on dispersion of directions of collagen fibres*) and spherical integration of contributions of individual fibres to the SEDF. It represents an extension of Holzapfel model with a dispersion parameter κ (0≤κ≤⅓) characterizing the dispersion of directions of collagen fibres. Two families of fibres are also considered here as follows:
The model gives good results for fibres with a not very high dispersion (κ → 0), while for high fibre dispersion (κ → 1/3) the error increases significantly. The reason is in the applied simplified spherical integration of contributions of the individual fibres to the strain energy assuming the same λ (and consequently the same φ) for all fibres in a family. To obtain more accurate results, it is necessary to consider individual fibre directions (and their individual stretch λ) which results in computational times higher by order**).
*) Gasser TC, Ogden RW, Holzapfel GA. Hyperelastic modelling of arterial layers with distributed collagen fibre orientations. J. R. Soc. Interface 2006; 3 : 15-35.
**) Skácel, Burša: Numerical implementation of constitutive model for arterial layers with distributed collagen fibre orientations. Computer methods in Biomechanics and Biomedical Engineering, Vol. 18/8 (2015), pp. 816-828.

## Slide 4: Parameters of direction dispersion of fibres
In literature there are two mutually interconnected parameters characterising the directions of fibres: the relation between the dispersion parameter κ and concentration parameter b is depicted in the figure; its mathematical formulation is rather complex:
*) Skacel P., Bursa J.: Comparison of constitutive models of arterial layers with distributed collagen fibre orientations. Acta of Bioengineering and Biomechanics, Vol 16/3 (2014) pp. 47-58.

## Slide 5: Relations between fibre waviness and their local and global directions
GOH model assumes two dispersed fibre families. Although they occur in histograms sometimes, this may be effect of collagen fibre waviness. The artificial figure with sinusoidal fibres gives bimodal histogram of local directions, while the GOH model requires the global directions (see red arrows), which are approximately 45°.

## Slide 6: Collagen fibre waviness
Bimodal shape of histograms of collagen fibre directions may be related to:
Two fibre families
One family of wavy fibres
For wavy collagen fibres two types of measures are used in literature:
Fibre waviness λ - stretch at which the fibre becomes straight
Straightness parameter Ps
Here lcurve represents the curvilinear length of the fibre and l represents the distance between its endpoints.
*) R. Rezakhaniha et al.: Experimental investigation of collagen waviness and orientation in the arterial adventitia using confocal laser scanning microscopy. Biomech Model Mechanobiol (2012) 11:461–473

## Slide 7: Model considering collagen fibre waviness
The pronounced strain stiffening of arterial tissues is caused by succesive engagement of wavy collagen fibres in the load transmission. Model Martufi*) (microfibre) aims at consideration of this effect using a bilinear probability function, describing a distribution of limit stretches of individual fibres (in a Neo-Hookean matrix).
*) Martufi G, Gasser TC: A constitutive model for vascular tissue that integrates fibril, fiber and continuum levels with application to the isotropic and passive properties of the infrarenal aorta. J Biomechanics 44 (2011) 2544–2550.

## Slide 8: Model Martufi ─ equations
The model introduces so called Cumulative Density Function (CDF – derivative of the probability density function of fibres). Under condition of incompressibility, the relation for first Piola-Kirchhoff stress T is as follows:
The applied triangular distribution function enables us to integrate per individual parts; in this way we obtain formulas for the first Piola-Kirchhoff stress T:
1) ..... for
2) ..... for
3) ..... for
4) ..... for
where: ;
The total contribution of fibres is then obtained by a spherical integration taking the distribution of directions of all collagen fibres into consideration.

## Slide 9: Model Martufi ─ constants
The model works with the following constants having their own physical meaning:
μ [Pa] ─ shear modulus (neo-Hookean model),
φ [°] mean angle of a fibre family,
k [Pa] ─ parameter characterizing the fibre stiffness (analogic to models Holzapfel 2000, Gasser 2006),
κ ─ parameter of dispersion of fibre directions in a family (0 ≤ κ ≤ 1/3),
λmin ─ fibre stretch, needed to straighten the least wavy fibres; beyond this limit the fibres start to bear load,
λmax ─ fibre stretch, needed to straighten the most wavy fibres; beyond this limit all the fibres bear some portion of the load.
.

## Slide 10: Predictive capability of Martufi model*)
The rings represent results of FE simulations of both tests with the model parameters obtained only from the uniaxial tension test of abdominal aorta (left) and with a very good prediction of the equibiaxial test (right).
*) Martufi G, Gasser TC: A constitutive model for vascular tissue that integrates fibril, fiber and continuum levels with application to the isotropic and passive properties of the infrarenal aorta. J Biomechanics 44 (2011) 2544–2550.
uniaxial tension test fit equibiaxial tension test prediction

## Slide 11: Limitations and modifications GHO model
There are two main limitations of all the presented structure-based models:
Without histological data the structural bases of the models is lost.
Histological analyses reveal a dominantly unidirectional (mostly circumferential) orientation of fibres with some dispersion; consequently the portion of fibres in the other (axial) principal direction is very low and cannot ensure any strain stiffening.
In contrast, the difference between stress-strain response of the arterial tissue in circumferential and axial direction is not so pronounced; typically some tens of percents. Thus the presented structure-based models cannot capture the real anisotropic responses of the tissue; there is no member in the SEDF function of GHO model enabling strain stiffening in the direction with less fibres (mostly axial). To overcome this limitation, a model with isotropic strain stiffening is needed. A suitable modification can be obtained with Yeoh model for the matrix as follows:
**) Skácel, Burša: Numerical implementation of constitutive model for arterial layers with distributed collagen fibre orientations. Computer methods in Biomechanics and Biomedical Engineering, Vol. 18/8 (2015), pp. 816-828.
Similar modifications are feasible also with other combinations of models.

## Slide 12: Model Holzapfel-Ogden*)
This model was formulated for passive behaviour of heart muscle tissue. Three ortogonal directions are defined by vectors f (direction of fibres), s (second direction in the sheet plane) and n (normal to the sheet). In the strain energy density function they are included as follows:
Here the first (isotropic) member represents contribution of the matrix, the second represents passive fibres, the third one is the contribution of lateral in-plane connections among fibres and the fourth member represents coupling term associated with directions f and s. Due to a pronounced strain stiffening all the members are exponential. The coupling (shear) invariant Isfs is defined as follows:
*) Holzapfel GA, Ogden RW. Constitutive modelling of passive myocardium: a structurally based framework for material characterization. Philosophical Transactions of the Royal Society A: Mathematical, Physical and Engineering Sciences. 2009;367(1902):3445-75.
This definition shows that the last (coupling) member may be non-zero only if the vectors f and s are not orthogonal, i.e. under shear deformation, which may be significant at heart muscle.